MUROBOND QUICK REFERENCE APPLICATION GUIDE

Murobond is a moisture cured product. This means application methods (and procedures immediately prior to and following application) are important. The following summarises a guide to good practice:

- Bare masonry surfaces: Surface should be thoroughly dampened (not glistening wet) before applying each coat. This is done by hosing the surface down with fresh water, and then allowing it to dry back until no glistening wet areas or dry patches are evident.

- Sealed surfaces: Murobond is applied directly to dry surface.

- Murobond should be applied to a cool surface away from direct sunlight. In hot or dry weather dampening immediately ahead of application may be necessary to cool the surface and maintain moisture.

- Murobond is mixed with water to the consistency of cream. Mix 3 parts powder to 2 parts water. Pot Life is approximately 2 - 3 hours.

- WSC: For parapet or garden walls, WSC is used. WSC is supplied in a concentrated form. This is diluted in the ratio 1 part WSC to 4 parts water. This WSC Solution is then used in place of water when mixing Murobond.

- Application: Murobond is applied by brush in random pattern maintaining a wet edge at all times. (Joining wet to dry will show). Large areas may need to be divided or involve more painters to achieve this. The special brushes available from Murobond are considerably faster than normal 100mm brushes and will wear longer.

- Clean up: water.

- Mist spraying the surface after application of each coat at least once is required to assist setting.   As a guide this is 2-4 hours after application (when the surface shows dry). It is recommended to mist spray the surface 2-3 times after each coat, however it is impossible to mist spray too many times. Leave a minimum of 24 hours between coats. The first coat should be lightly dampened immediately before applying the second coat.

- Murobond remains water sensitive until set, therefore the final coat  should be protected from rain and frost for a period of 48 hours and from mechanical abrasion for 7 days.

- Temperature. Murobond takes longer to set at colder temperatures and this should be allowed in setting times and protection periods. Murobond should not be applied at temperatures below 10C or above 35C

- Murobond Sealer is used over previously water-based painted surfaces (other than pure acrylic) before applying Murobond. It is supplied in ready to use form, clean up: water. Apply by spray, roller or brush.

The sealer can be overcoated as soon as it is touch dry, approx. 30-45 mins and should be overcoated within 7 days.

Surface does not require mist spraying before the first coat of Murobond over Sealer.

- Parapet walls: see WSC (above).

- Garden walls: see WSC (above).